## Slide 1: Nanotechnology is science, engineering, and technology conducted at the nanoscale, which is about 1 to 100 nanometer

## Slide 2: Nanomaterials
Pros
Different chemical nature
Different morphologies
High surface/volume ratio
High functionalizability
Easy interfaceability
Size/morphology dependent properties  tunability
Potential drawbacks
? Waste disposal
? Potential toxicity

## Slide 3: Nanomaterials employed in electrochemical sensor
Carbon based nanomaterials:
Nanotubes
Fullerenes
Graphene
Etc…
Graphene-like nanomaterials:
- e.g. Transition Metal Dicalchogenised (TMD)
Nanoparticles:
Metal nanoparticles
Metal Oxide nanoparticles

## Slide 4: CARBON NANOTUBES
CHARACHERISTICS
porous structure;
high mechanichal strenght;
easy to be modified;

## Slide 6: Carbon based nanomaterials (Carbon Black, CB)
Nano Carbon Black
Selectivity Sensitivity
Reproducibility
Improving separation performance
Electrocatalysis High surface
Resistance to fouling
Faster eletron transfer
CB compared with other nanomaterials:
Very low cost No synthesis
No impurities due to synthesis
Easily dispersible Large number of defect sites

## Slide 7
SPE CBNPs for direct analysis of carbamates in grain samples

## Slide 8
Electron transfer between a redox compound and an electrode (working electrode).
A redox compound is able to exchange electrons at a particular applied potential (applied potential depends on reference electrode)
Signal –current is used to detect/quantify
SENSOR
Amperometry – Voltammetry

## Slide 9
Amperometry: measurement of current at constant potential
Voltammetry: measument of current with varying potential
Scan rate

## Slide 10
Scan
rate
Electroanalytical-based strategies:
LINEAR SWEEP VOLTAMMETRY and CYCLIC VOLTAMMETRY
Reverse
Scan
LSW  NO REVERSE SCAN!!!
Red  Ox + ne-
Ox + ne-  Red
• ip,a: peak current of anodic oxidation,
• Ep,a: peak potential of anodic oxidation,
• ip,c: peak current of cathodic reduction,
• Ep,c: peak potential of cathodic reduction;
• △Ep= | Ep, a − Ep, c |: Peak-to-peak separation
(for ideal reversible 59/n mV)

## Slide 11
NERNST DIFFUSION LAYER
CAPACITIVE CURRENT
Electroanalytical-based strategies: voltammetry and amperometry
An electrolyte (salt) is necessary, to repress migration to the electrode driven by charge, the analyte should arrive to the electrode surface by diffusion or forced mass transport (pump, stirring) to have reproducible concentration signals
!!! PULSE METHODs !!!

## Slide 12
Electroanalytical-based strategies:
DIFFERENTIAL PULSE VOLTAMMETRIES and SQUARE WAVE VOLTAMMETRY
τ is the pulse period, tp is the pulse time, Estep is a potential step, △Ep is the pulse amplitude, ESW is the square wave amplitude, and △I is the resulting current.
Reversible species
Irreversible species

## Slide 13
Electroanalytical-based strategies:
DIFFERENTIAL PULSE VOLTAMMETRY

## Slide 14: Nano carbon black-based screen printed sensor for carbofuran, isoprocarb, carbaryl and fenobucarb detection: application to grain samples
1 mmol L−1 ferricyanide solution in 0.1 mol L−1 KCl of SPE CV performed at 5, 10, 25, 50, 75, 100,150 and 200 mV s−1
AFM
SEM
SPE
SPE-CB
SPE
SPE-CB
SPE
SPE-CB
SPE vs. SPE-CB electrochemical performance
SPE
SPE-CB

## Slide 16: SPE CBNPs for direct analysis of carbamates in grain samples
0,0E+00
3,0E-06
i (A)
2,0E-06
1,0E-06
4,0E-06
5,0E-06
0
200
400 µM 600
800
1000
Analyte | Linear range (µmol L- 1) | Regression equation (Y=am + b) | Coefficient of determinatio n (r2) | Detection limit (µmol L- 1) | Quantificatio n limit (µmol L-1)
Isoprocarb | 0.1-100 | y = 3E-08x + 5E- 09 | 0.9971 | 0.6 | 0.7
Carbofuran | 0.1-100 | y = 6E-08x - 1E- 08 | 0.9999 | 0.4 | 0.5
Carbaryl | 0.1-100 | y = 6E-08x + 2E- 08 | 0.9983 | 0.4 | 0.5
Fenobucarb | 0.1-100 | y = 3E-08x - 8E- 09 | 0.9996 | 0.6 | 0.7
Metolcarb | 0.1-100 | y = 6E-08x + 4E- 08 | 0.9980 | 0.3 | 0.4
SPE-CBNPs CMs Calibration, Reproducibility and Fouling resistance
Peak intensity (RSD, n=7): < 0.9 %
Peak potential (RSD, n =7): < 4,8 %
Inter electrode reproducibility (RSD, n=10): < 6.6 %
p.i and < 3,4 % p.E.
Fouling (peaks RSD):
DPV (n = 30, 250 µM) 96 % v.s.32 %
CV (n = 20, 500 µM) 94 % v.s 15 %
Isoprocarb Fenobucarb Metolcarb Carbaryl Carbofuran
(reaction medium: MEPS eluate after hydrolysis, 33 % ACN)

## Slide 17: Nano carbon black-based screen printed sensor for carbofuran, isoprocarb, carbaryl and fenobucarb detection: application to grain samples
Recoveries : 78–102%
Correlation: r= 0.952
Accuracy: relative error between 9.0% and −7.8%
Pesticide recoveries in grain samples

## Slide 18
Catechin 50 μM performed in phosphate buffer (10 mM + 0.1 M KCl at pH 7.0), scan rate of 50 mV s−1.
Nyquist plots of 5 mM Fe(CN)6 4-/3- in 0.1 KCl M performed with the bare SPE after each CVs scan
Della Pelle, F., Rojas, D., Scroccarello, A., Del Carlo, M., Ferraro, G., Di Mattia, C., Martuscelli, M., Escarpa, A., Compagnone, D. (2019). SENSOR ACTUAT B-CHEM, 296, 126651.
R ct
Electrochemical analytical drawback:
irreversible Passivation /low sensitivity for phenolic compounds
(occur after 1 scan; moreover: low sensitivity and repeatability. Impossible to perform a calibration)
...Catechin also adsorbs strongly on the electrode surface and the final oxidation product is not electroactive and blocks the electrode surface...
Janeiro, P., Brett, A.M.O. (2004). Analytica chimica acta, 518(1-2), 109-115.
SPE
Carbon Electrodes

## Slide 19: Transition Metal Dichalcogenides and their hybrid nanomaterials
Objective
MoS2 hybrids WS2 hybrids Group VI Transition Metal Dichalcogenides
Tendency to passivation (so called Fouling)
Nanomaterials
Transition Metal Dichalcogenides (TMDs)
TMDs are a family of 2D nanomaterials with general formula MX2 (M: Group 4-10 and X: S, Se and Te)
Arranged in a multilayered structure held by weak van der Walls forces
TMDs nanosheets easily prepared
by exfoliation
TMDs general structure
TMDs are poor conductive materials
Hinder its catalytic capabilities
Nanohybrids materials
Polyphenols electrochemical
sensing
Limitations using common electrodes

## Slide 20: Transition Metal Dichalcogenides and their hybrid nanomaterials
Nanohybrid electrode
CB-MoS2
CB-AuNPs-CT-WS2
Highly Conductive Nanomaterials
Carbon Black (CB)
Gold nanoparticles (Au-NPs-CT)
Dispersion and mix with exfoliated TMDs
Drop Casting
Electrode preparation methods
TMDs
Liquid Phase Exfoliation
Drop Casting
TMDs electrode
MoS2 MoSe2
WS2 WSe2

## Slide 21: Transition Metal Dichalcogenides and their hybrid nanomaterials
MoS2 hybrids
Objective WS2 hybrids
Group VI Transition Metal Dichalcogenides
D. Rojas, F. Della Pelle, M. Del Carlo, E. Fratini, A. Escarpa, D. Compagnone. Microchim. Acta. 186 (2019) 363.
CB–MoS2 nanohybrids shows an enhanced and synergistic electrocatalytic effect towards catechol
Electrochemical characterization
Catechol as representative redox moiety in food polyphenols
SPE CB MoS2
CB-MoS2
Cyclic Voltammetry (CV)
Catechol
Catechol moiety is present in highly antioxidant polyphenols
CB-MoS2

## Slide 22: Transition Metal Dichalcogenides and their hybrid nanomaterials
Cocoa
Catechin (CT)
Epicatechin (EP)
Epigallocatechin (EG)
MoS2 Nanohybrids
Objective WS2 Nanohybrids
Group VI Transition Metal Dichalcogenides
Correlation matrix: electrochemical sensor and well stablished analysis
CB-MoS2 | HPLC-UV | ABTS | AuNPs | FC
Olive Oil | 0.995 | - | - | -
Cocoa | - | 0.966 | 0.949 | 0.972
Application of CB-MoS2 electrochemical sensors to different food matrices
Olive oil
Oleuropein
(OLEU)
Hydroxytyrosol (HYT)
HO
HO
OH
OH
OH
O
O
COOCH3
O
O-GIu
CB-MoS
2
Catalytic effect extensive to complex structures

## Slide 23
S. TQ
S. + 0.25 μM EP
S. + 0.50 μM EP
SPE-CB-MoS2 has a regenerable electrode surface
59 cocoa samples consecutive analysis
Sample 12
Sample 5
Sample 1
DPV conditions:
pulse width 50 ms, pulse amplitude 20 mV.
Real sample analysis: n = 59 cocoa powder samples
Recoveries
Repeatability during n=59 sample analysis
From 94% to 103%
The sensor is exploitable for catechins determination
in complex samples
Signal recovery 99%
After n= 59 samples measured
RSD Ip,a < 0.9% and Ep,a< 5.2
10 µM epicatechin signal, obtained during the whole samples analysis
Della Pelle, F., Rojas, D., Scroccarello, A., Del Carlo, M., Ferraro, G., Di Mattia, C., Martuscelli, M., Escarpa, A., Compagnone, D. (2019). SENSOR ACTUAT B-CHEM, 296, 126651.
Notes: In order to evaluate if the catalytic effect, of the CB-MoS2 sensor, is observed even in more complex structures containing o-diphenols function. Therefore, we selected olive oil as case of study, with the most representative o-diphenols from olive oil: OLEU and HTYR. The behaviour observed for catechol and dopamine was also observed in OLEU and HTYR the highest signal was obtained using the CB-MoS2 electrodes. Those signals were evaluated using 5 different electrodes, and as you can see in the bars plot, the increment was significant. In addition, fouling resistance was improved compared to CB and Bare electrode and comparable to MoS2 itself. According to these results CB-MoS2 electrodes were chosen as the optimum ones for ortho-diphenols sensing.

## Slide 24: Transition Metal Dichalcogenides and their hybrid nanomaterials
WS2 Nanohybrids
Objective MoS2 Nanohybrids Group VI Transition Metal Dichalcogenides
F. Della Pelle, D. Rojas, F. Silveri, G. Ferraro, E. Fratini, A.
Scroccarello, A. Escarpa, D. Compagnone. Microchim. Acta. 187 (2020) 296.
WS2 nanohybrids electroc s)
hemical behavior towards different hydro - | xycinnamic acids (hCN SPE
- | SPE-WS2
- | SPE-CB
- | SPE-WS2/AuNP-CT
- | SPE-CB-WS2
- | Nanohybrid (SPE-CB-WS2/AuNP-CT)
hCNs general structure
R1=R2=OH Caffeic Acid
R1=R3=OCH3 R2=OH Sinapic Acid R2=OH Coumaric Acid
CB-AuNPs-CT-WS2
Synergistic electrocatalytic effect
Effective voltametric separation
Antifouling (97% signal retention (n=15))

## Slide 25: Biosensors based on enzyme inhibition

## Slide 27: Biosensor for organophosphate and carbamates pesticides (phytochemicals)
High acute toxicity (200.000 deaths/year in the 80s)
High chronic toxicity Moderate persistence
Mechanism of action:
inhibition of acetylcholinesterase (AChE)
Classical methods:
GC-NPD o GC-MS, LC-MS

## Slide 28: Scheme of the measurement
step 1
0.125 U/ml AChE
1 mL buffer + standard or sample
10’ incubation
Substrate (0.3 mM)
step 2
-50 mV vs Ag/AgCl
120’’
Is
RA %  100 * I 0
Is 
I0

## Slide 29: Working electrode reactions pathway
Screen printed electrode
ChOx layer
Electrochemical mediator (Prussian Blue)
Electrode surface (-50mV vs Ag/AgCl)
H2O2
Fe (III)  Fe (II)
Fe (III) + e-  Fe (II)
Acetylcholine + H2O  Acetic Acid +
Choline (AChE)
ChOx

## Slide 30
Diclorvos (organophosphate )
anticolinesterasic
Mechanism of AChE inhibition
E + C
E + CX
ECX
EC + X
k1
k2
k3
k-1
ki
E = enzyme; CX = carbamate or organophosphate; X = leaving group; Kd = k-1 / k1k2 carbamoylation or phosphroylation rate constant; k3 = decarbamylation or dephosphorilation rate constant; ki = bimolecular rate constant
Ability to detect at ng/mL;
Precision = 10%;
Total analysis time = 20 min

## Slide 31: Dichlorvos
Quantitative Usage for dichlorvos
The annual agricultural use of dichlorvos was estimated as 248,000/year during 90’ (ATSDR, 1997). Estimates done in late 1990s indicate that 60% of dichlorvos used worldwide was for plant protection, 30% was for public hygiene and vector control, and 10% to protect stored crops (WHO, 1999).
Solubility in water:
16 g/l
2,2-Dichlorovinyl dimethyl phosphate
Commercial formulation Didivane® is used as broad spectrum grain protectant insecticide.
Effective in controlling a wide range of insects that attack stored grain products.
It provides long-term protection against re-infestation from insects.
The European Union regulates the maximum adsmissible level in durum wheat at 2 mg/Kg (European Directive 2001/57/CE)

## Slide 32: Extraction + assay protocol
Sample extraction
Inhibition assay
1g
Whole grains Milled grains
2.5 or 5.0 ml
15 min.
filtration
Electrochemical measurement

## Slide 33: Matrix effect on the RA% and the I%
Experimental conditions:
Phosphate buffer pH 7.4, KCl 100 mM 10% matrix
AChE 0.125 U/ml, Ach 0.3 mM
200 ng/ml dichlorvos
Incubation time: 10 min.
50 ,0
45 ,0
40 ,0
35 ,0
30 ,0
25 ,0
20 ,0
15 ,0
10 ,0
5 ,0
0 ,0
PB S C v C laudio C v C iccio C v S vevo C v Iride C v sim eto
I% 200
ppb
I%
Experimental conditions:
Extraction in measuring buffer (1g/10ml)
140 ,0
120 ,0
100 ,0
80,0
60,0
40,0
20,0
0,0
bianco Cv. Cv. Cv. Svevo Cv. Iride Cv. C laudio C iccio S im eto
RA
%
RA%
Phosphate buffer pH 7.4, KCl 100 mM 10% matrix
AChE 0.125 U/ml, Ach 0.3 mM
Incubation time: 10 min.
RA%=100-(I0-Is/I0)*100

## Slide 34
Calibration of Dichlorvos in buffer and 10% matrix
Buffer


 
 

303.60
1124.83
 x  776.54  
1  e  
y   1035.26 
R=0.998
LOD= 8 ng/ml I50%=230 ng/ml




489 .98
566 .30
 x  755 .36  
1  e  
y   463 .20 




218 .04
83 .82
 x  276 .15  
1  e  
y   20 .86 
R=0.998
LOD= 130 ng/ml I50%=650 ng/ml
R=0.992
LOD= 45 ng/ml I50%=360 ng/ml
milled grains extract (10%)
LOD = 0.45 mg/Kg
LOD = 1.3 mg/Kg
0
20
40
60
80
100
120
0
-20
200
400
600
800
1000
1200
Dichlorvos (ng/ml)
Whole grains extract (10%)
I%
PBS
whole grain extract
milled grain extract
LOD = 2 x SD of no ihnibition measurement
I50% = 50% of inhibition

## Slide 35: Recovery from spiked samples (2 mg/Kg)
Experimental conditions:
Spiked samples
Extraction:1g whole grains sample in 10ml buffer AChE 0.125 U/ml, Ach 0.3 mM
Incubation time: 10 min.
n=5
100.0
80.0
60.0
40.0
20.0
0.0
Dichlorvos
Didivane
R%
Mean I%: 21.0±1.3
Mean recovery: 81.3 ±5.8
Mean I%: 19.2±1.2
Mean recovery: 79.5 ±3.5
Whole grains
Experimental conditions:
Spiked samples
Extraction:1g milled grains sample in 10ml buffer AChE 0.125 U/ml, Ach 0.3 mM
Incubation time: 10 min.
n=5
Dichlorvos
Mean I%: 9.3±1.9
Mean recovery: 81.3 ±16.1
Didivane
Mean I%: 10.2±2.1
Mean recovery: 89.5 ±19.0
I%LOD=8% !!
Milled grains

## Slide 36: Use of recombinant acetylcholinesterase (rAChE)
R=0.997
LOD= 0.045 ng/ml I50%=0.37 ng/ml
Buffer
milled wheat Extract 0.1%
R=0.995
LOD= 0.065 ng/ml I50%=0.85 ng/ml
120
100
80
60
40
20
0
0,0
1,0
2,0
3,0
4,0
5,0
ng/ml
I%
buffer
matrix extract 0.1%
rAChE: Mutant AChE from Drosophila melanogaster Clone B3 specific for dichlorvos
Fournier D et al. Protein Engineering, Vol. 15, No. 1, 43-50, January 2002
M e a n I %  SD
C a l c . C o n c .
m e a s u r i n g s o l n . ( n g / m l )
M e a n r e c o v e r y  SD ( m g / K g )
70 . 2  4 .5
1 .5
75 . 0  4 .8
Di c h lo r v o s ( n = 3 )
D i d i v a n e ( n = 3 )
69 . 2  7 .3
1 . 4 5
72 . 5  7 .6
LOD= 0.065 mg/Kg
Milled wheat Extract 0.1%

## Slide 37: Paper can… Store Filter React
Paper as substrate
Drawbacks… Reagents diffusion… Electrical noise! 
An hydrophobic barrier
is needed…
Sustainable
Available
Low-cost

## Slide 38: From Paper to E-Paper
Few and easy steps

## Slide 39
Hydrophilicity matters
… also the cost!

## Slide 40: It depends on what you need and you have!
Not just wax printing

## Slide 41: Which E-Paper?
Porous
Non porous
Anyway, paper is the substrate… we need to make these strips ad-hoc

## Slide 42: Office paper for ethanol
S. Cinti et al. Anal. Chim. Acta 960 (2017) 123-130

## Slide 43: Detection mechanism
Office paper
Carbon Black
Prussian Blue
Alcohol oxidase

## Slide 44: Optimization
Calibration curve
Accordance with label
LOD = 0.5 mM
Linear range up to 10 mM
RSD = 8 %

## Slide 45: 3-D paper origami for pesticides
Paraoxon, 2,4-dichlorophenoxyacetic acid, and atrazine by inhibition of
butyrylcholinesterase, alkaline phosphatase, and tyrosinase
F. Arduini et al. Biosens. Bioelectron. (2018) DOI:10.1016/j.bios.2018.10.014
Filter paper+ office paper

## Slide 47: E.g. paraoxon detection
LOD = 2 ppb
Linear range up to 30 ppb
RSD = 11%
Real sample: River water Linear up to 30 ppb
Recoveries: 90 and 88%
(10 and 20 ppb)

## Slide 48: Paper + laser induced graphene + electrochemistry
CARBARYL
MRL 0.5 mg/Kg
MRL 0.8 mg/Kg
MRL 0.1 mg/Kg
3D POP-UP device

## Slide 49
Graphene
Laser induced graphene
Laser induced graphene

## Slide 50: POP UP fabrication
100°C
10 min
Vinyl stencil
Cutter printer
Nitrocellulose
Ag ink
Graphene oxide water solution
Vacuum filtration
CO2 laser
1- engraving
2- cutting
GO
rGO

## Slide 51: POP UP fabrication
100°C
15 min
Press- transfer
Grey dielectric paste
Wax printer
Chromatographic paper
2
CO laser
7 cm
4 cm
Interlocking tabs
Sampling window
Supporting arms
Sensor
housing
LP: 6.6 W
LS: 0.075 m s-1
Wax percolation 100°C, 10 min
tons
min

## Slide 52: Measure set up
1- 3D configuration
5 drops of 15 μL
MeOH evaporation
CBR concentration
3- Hydrolysis
NaOH 60 mM
4- Neutralization
NaH2PO4 30 mM
5- Measure
2- Sample loading
DPV
50 ms pulse width, 50 mV modulation amplitude, and 25 mV s -1 scan rate
Carbaryl
1-Naphtol

## Slide 53: Analytical performances
0.0 0.1 0.2 0.3 0.4
E (V)
0.2 μA
Solid line  CBR hydrolyzed on the POP-UP device
Dashed line  1-NP used as control
5 μM and 25 μM
Quantitative
hydrolysis
LR: 1.5 - 33 μM
R2= 0.9950
RSD ≤ 10%, n=3
LOD: 0.4 μM
LOD < MRL in grains

## Slide 54: Sample analysis
Soft wheat 1 (SW1) Soft wheat 2 (SW2) Durum wheat (DW) Kamut (KM)
Barley (BR)
5 mg in 10 mL of methanol
Extraction under orbital stirring for 5 min at 4000 g
CBR fortification at:
0.5 MRL (1.7 μM)
1 MRL (3.5 μM)
1.5 MRL (5.2 μM)
Carbaryl MRL in grains: 3.5 μM
0.0 0.1 0.2 0.3 0.4
E (V)
0.02 μA
1.5 MRL
1 MRL
0.5 MRL
Recovery: 93-108% (RSD ≤ 6%, n = 3)
Interferents

## Slide 55
Acido lattico, monouso (Sens-Lab)
Etanolo
Multianalita (zuccheri, alcol, acidi organici) Universal Sensor
Glucose, Lactate, Ethanol, Methanol, Ammonia, Glycerol, Sucrose, Lactose and Glutamine

## Slide 56
english version